台南市仁德區三甲里 59-1 號

59-1,San Chia, Jen Te, Tainan City 71702, Taiwan TEL: 886-6-266-5000 FAX: 886-6-266-5555~7

WONDERLOY®  PC-540A

PC/ABS alloy, non-halogen Flame Retardant

PROPERTIES	CONDITION	VALUE	UNIT	METHOD

PHYSICAL

Melt Flow Index

Spiral Flow Length

Specific Gravity

Mold Shrinkage

Rockwell Hardness

CLTE

MECHANICAL

Tensile Strength @ Yield

Tensile Strength @ Break

Tensile Elongation @ Yield

Tensile Elongation @ Break

Flexural Strength

Flexural Modulus

Izod Impact（1/8”）

THERMAL

Heat Distortion Temp.（unannealed）

| 260℃/2.16kg | 20 | g/10min | ASTM D-1238 |
| --- | --- | --- | --- |
| 260℃,2mm | 40 | cm | Chimei method |
| V:50%, P:50% |  |  |  |
| 23℃ | 1.18 | --- | ASTM D-792 |
|  | 0.4~0.6 | % | ASTM D-955 |
| 23℃ | R-119 | --- | ASTM D-785 |
| Flow:23-55℃ | 8.00E-05 | cm/cm/℃ISO11359-2 |  |

| 50mm/min | 600 | kg/cm2 | ASTM D-638 |
| --- | --- | --- | --- |
| 50mm/min | 550 | kg/cm2 | ASTM D-638 |
| 50mm/min | 4 | % | ASTM D-638 |
| 50mm/min | 100 | % | ASTM D-638 |
| 1.3mm/min | 900 | kg/cm2 | ASTM D-790 |
| 1.3mm/min | 25000 | kg/cm2 | ASTM D-790 |
| Notched, 23℃ | 45 | kg-cm/cm | ASTM D-256 |

| 3.2mm,1.82Mpa | 86 |  |  |
| --- | --- | --- | --- |
| 120℃/hr |  | ℃ | ASTM D-648 |
| 6.4mm,1.82Mpa | 95 |  |  |

120℃/hr

Vicat Softening Temp.（unannealed）

ELECTRICAL

Dielectric Constant

Volume Resistivity

Surface Resistivity

FLAMMABILITY

UL Recognized, 94V-0 Flame Class Rating

UL Recognized, 94-5VB Rating

UL Recognized, 94-5VA Rating

| 1kg, 50℃/hr | 108 |
| --- | --- |
| 5kg, 50℃/hr | 101 |
| 1MHz | 3.1 |
| -- | 3.9E+17 |
| -- | 2.9E+17 |
|  | 1.5 mm |

2.0 mm

3.0 mm

- ASTM D-1525

--	IEC 60250

Ohm*m	IEC 60093

Ohm	IEC 60093

UL-94

UL-94

UL-94

台南市仁德區三甲里 59-1 號

59-1,San Chia, Jen Te, Tainan City 71702, Taiwan TEL: 886-6-266-5000 FAX: 886-6-266-5555~7

| PROCESSING PARAMETERS |  |  |
| --- | --- | --- |
| Drying Temperature | 80 | ℃ |
| Drying Time | 3~4 | Hrs |
| Barrel Temperature | 240~280 | ℃ |
| Mold Temperature | 50~100 | ℃ |

All figures listed here is for reference, not guaranteed.

Final revised date：2014/12

Unless otherwise stated the results shown in this test report refer only to the sample(s) tested. This test report cannot be reproduced, except in full, without prior written permission of the Company。Attention is drawn to the limitation of liability, indemnification and jurisdiction issues defined therein. Any holder of this Test Report is advised that information contained hereon reflects the Company’s findings at the time of its intervention only and within the limits of Client’s instructions, if any. The Company’s sole responsibility is to its Client and this document does not exonerate parties to a transaction from exercising all their rights and obligations under the transaction documents. Any unauthorized alteration, forgery or falsification of the content or appearance of this document is unlawful and offenders may be prosecuted to the fullest extent of the law.